Included on this page are Lubri-Tech paint charts.  Lubri-Tech is no longer in business.

An expanded version of this chart and Triple paint codes are available in this [spreadsheet](http://kawatriple.com/paint.xlsx).

*Paint Application Chart*

*(Lubri-Tech, 1973-78)*

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **Model** | **Kawasaki Motorcycle Factory Color** | **First Coat**  **(Base Coat)** | **Second Coat** | **Third Coat** |
| H1A | Harbor Blue | White Pearl  UC-16-300 | Flair Silver Pearl  TC-16-100 | 72 Pearl Candytone Blue  KP-16-502 |
| S1, S2 | Pearl Candytone Red | White Pearl  UC-16-300 | Flair Silver Pearl  TC-16-100 | 72 Pearl Candytone Red  KP-16-201 |
| H1B/C, S1A, S2A | Pearl Candytone Orange | White Pearl  UC-16-300 | Gold Pearl  TC-16-600 | 72 Pearl Candytone Orange  KP-16-202 |
| H2, S2A | Pearl Candytone Blue | White Pearl  UC-16-300 | Flair Silver Pearl  TC-16-100 | 72 Pearl Candytone Blue  KP-16-502 |
| S1A, H2A | Candy Gold | Candy Silver  UC-16-100 |  | Candy Gold  KC-16-600 |
| H1D | Burnt Lime | Gloss Black  BG-16-400 | Flair Silver Pearl  TC-16-100 | Candy Lime  KC-16-900 |
| H1D | Candy Lime | White Pearl  UC-16-300 | Flair Silver Pearl  TC-16-100 | Candy Lime  KC-16-900 |
| H2C, S3A | Candy Super Red | Dark Gray Primer  GP-16-301 | MIO Basecoat  UC-16-111 | Garnet Red Candy  KC-16-201 |
| S3A | Candy Green | Dark Gray Primer  GP-16-301 | MIO Basecoat  UC-16-111 | Peacock Green Candy  HC-16-905 |
| H1F | Candy Sky Blue | Dark Gray Primer  GP-16-301 | MIO Basecoat  UC-16-111 | Bright Sky Blue Candy  KC-16-504 |
| H1F | Candy Gold | Dark Gray Primer  GP-16-301 | MIO Basecoat  UC-16-111 | Candy Gold  HC-16-600 |
| S1C | Candy Halibut Blue | Candy Silver  UC-16-100 |  | Blue Candy  HC-16-500 |
| KH500 | Deep Burgandy | Mandarin Orange  KS-16-201 | MIO Basecoat  UC-16-111 | Candy Matador Red  HC-16-205 |
| KH500 | Copper | Mandarin Orange  KS-16-201 | MIO Basecoat  UC-16-111 | Candy Gold  HC-16\_600 |
| KH400-A3 | Dark Green | Mandarin Orange  KS-16-201 | MIO Basecoat  UC-16-111 | Brilliant Lime Candy  KC-16-901 |
| KH400-A3 | Orange | Mandarin Orange  KS-16-201 | MIO Basecoat  UC-16-111 | 72 Pearl Candytone Orange  KP-16-202 |
| KH250 | Candy Super Red Custom | White Pearl  UC-16-300 | Custom Silver  UC-16-101 | Super Candy Red  KC-16-202 |
| KH400-A4 | Candy Emerald Green | Light Gray Met  UC-16-118 |  | Emerald Green Candy  KC-16-903 |
| H2C | Candy Purple | Dark Gray Primer  GP-16-301 | MIO Basecoat  UC-16-111 | Candy Purple  HC-16-500 |















